՛՛ARMENIA՛՛ INTERNATIONAL AIRPORTS՛՛ CJSC

MAINTENANCE

DESCRIPTION

"Zvartnots" airport

Aerodrome pavement repairing

The space between Apron No1 (10-14 parking) and T-3 (under galleries)

YEREVAN

2023թ․

- PLANNED WORKS DESCRIPTION

The renovation works include:

- Implementation of asphalt-concrete pavement milling keeping the slopes

- After milling implementation of the huge cracks filling with aerodrome sealant, and geo-grid laying

- After milling implementation of asphalt-concrete pavement pits repairing

- Implementation of asphalt-concrete pavement renovation with 6cm average thickness

- Marking works implementation

- REQUIREMENTS FOR IMPLEMENTATION OF WORKS

- All construction and repair works must be implemented in accordance with the norms of the Republic of Armenia, as specified in the description, safety rules, as well as the requirements of CN&R (Construction norms and rules) 2.05.08-85, ICAO Annex 14, Part 1.

- Asphalt-concrete and concrete pavements cutting must be done with cutting equipment having a diamond disc.

- Implement asphalt-concrete pavement quality milling through the milling machine ensuring the necessary slopes. For ensuring the slopes, it is necessary to provide milling with the help of leveling pegs and copying wire.  The distance between pegs should be no more than 10m. Milling must be done by the “NON-STOP” method. The milled asphalt-concrete needs to be transferred to a location designated by the airport. During asphalt concrete milling there appear damaged areas between the layers of existing asphalt concrete, which must be demolished with a milling machine and a compressor.

- First the joints and cracks must be cleaned with compressed air and then filled with airfield sealant with special cracks filling machine.

- Before filling the bitumen emulsion, clean the surface from old sealant residues, stones and dust by sweeping with a Bobcat universal mechanism and compressed air. Vacuum cleaners equipped with brushes and a vacuum air drive system can also be used for cleaning works;

- Before filling bitumen emulsion, the surface of the asphalt concrete pavement must be dry and clean. The bitumen emulsion must be heated. Filling of bitumen emulsion with a computer-controlled bitumen spreading machine;

- Asphalt concrete mix must comply with GOST 9128-2013 A- type, I- grade. The temperature of the mixture during spreading should be 140oC-160oC. The surface of the asphalt concrete pavement should be smooth and homogeneous, without uneven areas, provided with the necessary compaction. At the end of the asphalt concrete pavement, a wooden or metal beam should be installed and fixed in the transverse direction. Compaction of the spread asphalt concrete layer should be carried out at a temperature of not less than 120oC. At lower temperatures, the implementation of the asphalt concrete layer is not allowed; the asphalt concrete is subject to removal: For the asphalt concrete mix brought in each shift, it is necessary to submit a laboratory test document that will confirm its compliance with the presented requirements.

The pavement smoothness must meet the requirements of ICAO Annex 14, Appendix- A, and Clause - 5. In order to obtain the maximum quality of laying asphalt concrete layers, the works should be performed with a 4-6 m wide asphalt paver, which is equipped with lighting, a slope and level detection system, and a 2D leveling system. In order to secure slopes, it is necessary to provide milling with the help of leveling pegs and copying wire. The distance between pegs should be no more than 5m.

For asphalt concrete layer compaction, should be used the rollers with an oscillating mechanism (off-center vibration) weighing 6-8 and 10-12 tons, and for pneumo - rollers weighing 20-25 tons.

- Asphalt concrete mixture should be modified with polymer additives. For modification, it is necessary to apply additives with the following parameters: - increased strength; reduction of cumulative deformations; improvement of the fatigue characteristics of the mix (SUPERPLAST or similar)

- Increasing the adhesion of stone materials and bitumen, improving the characteristics of bitumen (ITERLENE IN/400-L or similar).

Depending on the weather conditions, it is necessary to apply an additive with the following parameters:

- Installation and compaction of asphalt concrete mixtures at low temperatures, and increasing the comfort of placing asphalt concrete mix and transporting the mix over long distances (ITERLOW T or similar) in case of low temperatures.

For the modification, plan for equipping the asphalt concrete plant with appropriate equipment.

The contractor must submit a document for the selection of the asphalt concrete components and agree with the airport's Maintenance Department.

- It is necessary to cut the joints of the asphalt concrete pavement in the joints filling areas with the perimeter of the previous day's pavement and treat it with bitumen in order to ensure quality joints filling of the asphalt concrete pavements. Project marks must not be disturbed at the cutting site.

At the end sections of the new asphalt concrete pavement, carried out during each shift, where the leveling rollers protrude from the newly laid asphalt-concrete pavement onto the milled surface, the cracks appear – that means temporary slopes. The appeared cracks should be milled with a width of 1m and a depth of 9cm from that area before continuing the laying of the new asphalt-concrete pavement.

- It is necessary to repair the manholes in the area under repair, by demolishing or raising the concrete walls as necessary, ensuring the required mark of the manhole cover.

- Manholes must be implemented of Concrete M-300, П-3, F200, GOST 7473-94: It is necessary to take care of the concrete with 7-days providing favorable fastening conditions. Fastening should be carried out in accordance with the current norms and rules. Armature AIII class, GOST 5781-82. After getting 28-days strength of the concrete, it is necessary to waterproof the walls and slab of the manhole with TECNONICOL №24 or similar bituminous polymer mastic. To accelerate the strength of concrete and ensure frost resistance, it is necessary to use appropriate additives in agreement with AIA.

- It is necessary to remove the existing reinforced concrete slabs in the repair area carefully, without damaging the adjacent slabs, and install new ones.

- It is necessary to transport the construction waste to the appropriate permitted landfill or another place designated by the airport, submit a certificate from the specified landfill or community;

Marking works should be carried out with water-based paints intended for aerodromes (the contractor should present certificates of origin and quality)

- Used  GOST and NORMS

- ICAO appendix 14, part 1, “Aerodromes”

- ICAO doc 9157 AN/901., “Aerodrome Design Manual”

- CN&R 2.05.08-85, “Aerodromes”

- CN&R 3.06.06-88, “Aerodromes”

- CN&R III-4-80* Construction Safety

- GOST 7473-94,” Concrete mixtures. Specifications”

- GOST 5781-82, “ Steels for concrete reinforcement ”

- GOST 8736-93, “Sand for construction works. Specifications”

- GOST 8267-93 ‘’Crushed stone and gravel of solid rocks for construction works. Specifications’’

- GOST9128-2013, “Asphaltic concrete and polymer asphaltic concrete mixtures, asphaltic concrete and polymer asphaltic concrete for roads and aerodromes. Specifications”

- GOST 22245 – 90, “Viscous petroleum road bitumen. Specification”

- GOST 17.4.3.04-85 ‘’Nature protection. Soils. Classification of chemicals for pollution control’’

- REQUIREMENTS FOR MATERIALS

1. Concrete M-300, P-3, F200, GOST 7473-94 (GOST 7473-94);

2. Armature AIII class, GOST 5781-82 (GOST 5781-82);

3. Asphalt-concrete mixture A –type, I mark GOST 9128-2013;

4. Gravel basalt: breakability index 1200, abrasion index I1, frost resistance F50

5. Sand washed, quartz or crushed - medium size;

6. Bitumen corresponding to PRB -60/90 (БНД 60/90) mark

- penetration 0,1mm

250C                  61-90

00C                    not less 20

- softening point 0C

not less 47

- elasticity, cm

250C                  not less 55

00C                   not less 3.5

- softening point 0C

not more than -15

- flash point, 0C

not less 230

- softening point change after heating 0C

not more than 5

- penetration index

-1.0 up to +1.0

7. Filler – carbon

8. Sealant for joints filling SIKAFLEX PRO-3 (Sika-flex PRO-3) or similar

9. Fiberglass Geo-grid 100/100-40 (TSGM100/100-40, Fiberglass geo-grid 100-100KN) corresponding to the quality, intended for aerodromes

10. Water-based paints certified for aerodrome marking:

* In order to fully familiarize yourself with the requirements for the implementation of works and the quality of materials, it is necessary to study the description of the implementation of the works.