՛՛ARMENIA՛՛ INTERNATIONAL AIRPORTS՛՛ CJSC

MAINTENANCE

DESCRIPTION

"Zvartnots" airport

TWY ՛՛B՛՛- phase I, Pavement repairing works

YEREVAN

2023թ․

- PLANNED WORKS DESCRIPTION

TWY ՛՛B՛՛-Pavement phase I repairing works include:

- In bearing part

- Implementation of asphalt-concrete  pavement milling due to the project

- After milling implementation of the huge cracks filling with aerodrome sealant, and geo-grid laying

- After milling implementation of asphalt-concrete  pavement pits repairing

- Implementation of asphalt-concrete  pavement renovation with 10 cm average thickness due to the project

- In shoulders

- Demolition of the existing cover and construction of a new one according to the drawing;

- ground elements joints filling works with the correction of slopes

- existing lighting system repairing

- implementation of new passes of engineering communications

- marking works implementation

- REQUIREMENTS FOR IMPLEMENTATION OF WORKS

All construction and repair works must be implemented in accordance with the norms of the Republic of Armenia, as specified in the description, safety rules, as well as the requirements of CN&R (Construction norms and rules) 2.05.08-85, ICAO Annex 14, Part 1.

- Before starting the works, it is necessary to carry out temporary marking, removing it (mark with black paint) after the completion of the works.

- Asphalt-concrete and concrete pavements cutting must be done with cutting equipment having a diamond disc.

- Implement asphalt-concrete  pavement quality milling through the milling machine ensuring the necessary slopes. For ensuring the slopes, it is necessary to provide milling with the help of leveling pegs and copying wire.  The distance between pegs should be no more than 10m, in slopes 5m. Milling must be done by the “NON-STOP” method. The milled asphalt-concrete  needs to be transferred to a location designated by the airport.

During asphalt concrete milling there appear damaged areas between the layers of existing asphalt concrete, which must be demolished with a milling machine and a compressor.

- First, the joints and cracks must be cleaned with compressed air; then filled with airfield sealant with special cracks filling machine. It is necessary to install Geo-grid with 1.5m width and CNandR 100/100-40 (Fiberglass geogrid 100-100KN) quality and fix it. Fixation steps must be 8-10 fixation/1m2: Fixation should be done with concrete nails with special screws.

- Before filling the bitumen emulsion, clean the surface from old sealant residues, stones and dust by sweeping with a Bobcat universal mechanism and compressed air. Vacuum cleaners equipped with brushes and a vacuum air drive system can also be used for cleaning works;

- Before filling bitumen emulsion, the surface of the asphalt concrete pavement must be dry and clean. The bitumen emulsion must be heated. Filling of bitumen emulsion with a computer-controlled bitumen spreading machine;

- Asphalt concrete mix must comply with GOST 9128-2013 A- type, I- grade. The temperature of the mixture during spreading should be 140oC-160oC. The surface of the asphalt concrete pavement should be smooth and homogeneous, without uneven areas, provided with the necessary compaction. At the end of the asphalt concrete pavement, a wooden or metal beam should be installed and fixed in the transverse direction. Compaction of the spread asphalt concrete layer should be carried out at a temperature of not less than 120oC. At lower temperatures, the implementation of the asphalt concrete layer is not allowed; the asphalt concrete is subject to removal: For the asphalt concrete mix brought in each shift, it is necessary to submit a laboratory test document that will confirm its compliance with the presented requirements.

The pavement smoothness must meet the requirements of ICAO Annex 14, Appendix- A, and Clause - 5. In order to obtain the maximum quality of laying asphalt concrete layers, the works should be performed with a 4-6 m wide asphalt paver, which is equipped with lighting, a slope and level detection system, and a 2D leveling system. In order to secure slopes, it is necessary to provide milling with the help of leveling pegs and copying wire. The distance between pegs should be no more than 5m.

For asphalt concrete layer compaction, should be used the rollers with an oscillating mechanism (off-center vibration) weighing 6-8 and 10-12 tons, and for pneumo - rollers weighing 20-25 tons.

- Asphalt concrete mixture should be modified with polymer additives. For modification, it is necessary to apply additives with the following parameters;

- increased strength; reduction of cumulative deformations; improvement of the fatigue characteristics of the mix (SUPERPLAST or similar)

- increasing the adhesion of stone materials and bitumen, improving the characteristics of bitumen (ITERLENE IN/400-L or similar).

Depending on the weather conditions, it is necessary to apply an additive with the following parameters:

- Installation and compaction of asphalt concrete mixtures at low temperatures, and increasing the comfort of placing asphalt concrete mix and transporting the mix over long distances (ITERLOW T or similar) in case of low temperatures.

For the modification, plan for equipping the asphalt concrete plant with appropriate equipment.

The contractor must submit a document for the selection of the asphalt concrete components and agree with the airport's Maintenance Department.

- It is necessary to cut the joints of the asphalt concrete pavement in the joints filling areas with the perimeter of the previous day's pavement and treat it with bitumen in order to ensure quality joints filling of the asphalt concrete pavements. Project marks must not be disturbed at the cutting site.

At the end sections of the new asphalt concrete pavement, carried out during each shift, where the leveling rollers protrude from the newly laid asphalt-concrete  pavement onto the milled surface, the cracks appear – that means temporary slopes. The appeared cracks should be milled with a width of 1m and a depth of 9cm from that area before continuing the laying of the new asphalt-concrete  pavement.

- The cement-fixed gravel mixture must meet the requirements of GOST 23558-94 (the size of the largest gravel is not more than 40 mm), must be installed in two layers, each layer with a thickness of no more than 15-20 cm, the cost of cement will be 80 kg/m3.  A polyethylene sheet should be spread over the sand before placing the mix. Depending on the weather conditions, the mix should be treated within 2-4 days. Crushed-stone layer must be compacted with rollers, but where it is not possible to provide roller there must be used vibro-plate or vibro-compactor, ensuring the necessary depth.  Surface must be smooth without pits and hills.  Mix compound must be accepted due to the table

| Granular maximum size | Total residue on the sieve in %, on the specified sieve size, mm |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 40 | 20 | 10 | 5 | 2.5 | 1.25 | 0.63 | 0.315 | 0.14 | 0.05 |
| 40 | up 10 | 20-40 | 35-65 | 50-80 | 60-85 | 70-90 | 75-95 | 80-97 | 85-98 | 87-100 |

- It is necessary to demolish or dismantle the non-operational manholes existing in the ground, and fill the pits with soil and compact them with layers up to 30 cm thick. Dismantling of manhole covers should be done carefully without damaging them, then load and transfer in the airport area. Before dismantling manhole covers on the artificial pavement, it is necessary to cut the cover along the perimeter of the manhole cover.

- It is necessary to replace the existing iron-concrete cover slabs of the manholes in the ground part with F-900 type metal inlet, iron-concrete covers, M-300 concrete brand.  If necessary, demolish the walls of the existing manholes and adjust their markings to the norms of ground fillings. It is necessary to make iron-concrete frame with a thickness of 10-20 cm along the perimeter of the raised manholes walls. It is necessary to implement iron-concrete walls partial demolition along the perimeter of the drop-down manholes walls, then implement cement-sand plastering between covers and walls with an average thickness of 3cm. demolition works must be realized mechanically and by the compressor.  If necessary and in those areas where it is not possible to use the mechanism, the works must be implemented manually. iron-concrete manholes walls demolition must be implemented with the utmost care, without damaging the lower parts and reinforcement.  According to the model drawing and the study carried out on the site, it is necessary to prepare the reinforced iron-concrete oncrete covers of the manholes in advance.

- Manholes must be implemented of Concrete M-300, П-3, F200, GOST 7473-94: It is necessary to take care of the concrete with 7-days providing favorable fastening conditions. Fastening should be carried out in accordance with the current norms and rules. Armature AIII class, GOST 5781-82. After getting 28-days strength of the concrete, it is necessary to waterproof the walls and slab of the manhole with TECNONICOL №24 or similar bituminous polymer mastic. To accelerate the strength of concrete and ensure frost resistance, it is necessary to use appropriate additives in agreement with AIA

- Before dismantling the polyethylene pipes of the Lighting system, it is necessary to implement sand preparatory layer laying and compaction, install the pipes; cover the pipes with sand and concrete the parts covered with asphalt-concrete  cover. The pass ability of the polyethylene pipes must be ensured. It is necessary to plan cast wire inside of the polyethylene pipes.

- To install new polyethylene pipes inside the manhole walls, in case of need combine them with existing pipes, ensuring the pass ability.

- Demolish runway iron-concrete bases of the light boards mechanically and install new iron-concrete bases. The levels must correspond to the implemented surface levels.

- It is necessary to transfer the additional ground and construction waste to the appropriate permitted landfill or other place designated by the airport, submit a certificate from the specified landfill or community

- Marking works should be carried out with water-based paints intended for aerodromes (the contractor should present certificates of origin and quality)

- Used  GOST and NORMS

- ICAO appendix 14, part 1, “Aerodromes”

- ICAO doc 9157 AN/901., “Aerodrome Design Manual”

- CN&R 2.05.08-85, “Aerodromes”

- CN&R 3.06.06-88, “Aerodromes”

- CN&R III-4-80* Construction Safety

- GOST 7473-94,” Concrete mixtures. Specifications”

- GOST 5781-82, “ Steels for concrete reinforcement ”

- GOST 8736-93, “Sand for construction works. Specifications”

- GOST 8267-93 ‘’Crushed stone and gravel of solid rocks for construction works. Specifications’’

- GOST9128-2013, “Asphaltic concrete and polymer asphaltic concrete mixtures, asphaltic concrete and polymer asphaltic concrete for roads and aerodromes. Specifications”

- GOST 22245 – 90, “Viscous petroleum road bitumen. Specification”

- GOST 17.4.3.04-85 ‘’Nature protection. Soils. Classification of chemicals for pollution control’’

- REQUIREMENTS FOR MATERIALS

1. Concrete M-300, P-3, F200, GOST 7473-94 (GOST 7473-94);

2. Armature AIII class, GOST 5781-82 (GOST 5781-82);

3. Asphalt-concrete  mixture A –type, I mark GOST 9128-2013;

4. Gravel basalt: breakability index 1200, abrasion index I1, frost resistance F50

5. Sand washed, quartz or crushed - medium size;

6. Bitumen corresponding to PRB 60/90 (БНД 60/90) mark

- penetration 0,1mm

250C                  61-90

00C                    not less 20

- softening point 0C

not less 47

- elasticity, cm

250C                  not less 55

00C                   not less 3.5

- softening point 0C

not more than -15

- flash point, 0C

not less 230

- softening point change after heating 0C

not more than 5

- penetration index

-1.0 up to +1.0

7. filler – carbon

8. Sealant for joints filling SIKAFLEX PRO-3 (Sika-flex PRO-3) or similar

9. Fiberglass Geo-grid 100/100-40 (FGTS100/100-40, Fiberglass geo-grid 100-100KN) corresponding to the quality, intended for aerodromes

10. Water-based paints certified for aerodrome marking:

* In order to fully familiarize yourself with the requirements for the implementation of works and the quality of materials, it is necessary to study the description of the implementation of the works.